<<Company Name>> ACM Product Chart

| Product | Use | Approx. % of asbestos |
| --- | --- | --- |
| Loose | Mattresses/quilts for fire stopping or sound insulation | 100 |
| Sprayed coating | Dry or wet applied, anti-condensation or acoustic insulation, structural fire protection | 55-85 |
| Thermal insulation Lagging, pre-formed sections. Tapes, ropes, paper, felting, blankets | Of pipes, boilers, pressure vessels, calorifiers | 6-85 |
| Asbestos boards |  |  |
| Millboard | Fire protection, heat and electrical insulation | 67-97 |
| Insulating board | Fire breaks, infill panels, partitions, ceilings, ceiling tiles, linings to roofs and walls, external canopies and porch linings | 16-40 |
| Paper, felt, cardboard, electrical and heat insulation | Reinforcement and linings of other products | 100 |
| Textiles |  |  |
| Ropes and yarns | Jointing and packing, boiler, oven and flue seating – plaited tubing in electric cable | 100 |
| Cloth | Fire blankets, mattresses, curtains, gloves | 100 |
| Gaskets and washers | Hot water boilers to industrial power and chemical plant | 90 |
| Strings | Seals to hot water radiators | 100 |
| Friction products |  |  |
| Rein-based materials | Brakes and clutch plates in machinery and lifts | 30-70 |
| Drive and conveyor belts | Engines and conveyors | 30-70 |
| Cement products |  |  |
| Profiled sheets | Roofs, wail cladding, permanent shuttering | 10-15 |
| Semi-compressed flat sheet and partition board | Bath panels, soffits, walls, ceiling linings, weather boarding, composite panels for fire protection or as base for decorative facings | 10-25 |
| Fully compressed flat sheet for slates, tiles, board | Worktops, imitation roof slates | 10-15 |
| Pre-formed moulded and extruded products | Troughs and conduits, cisterns and tanks, drain pipes, flues, rainwater goods, windowsills and reveals, fascias, soffits, ducts, copings, promenade tiles and early imitation slates | 10-15 |
| Other encapsulated materials |  |  |
| Textured coatings | Decorative coatings on walls and ceilings | 3-5 |
| Bitumen products | Early forms of roofing felt, gutter linings and flashings, DPC, mastic and adhesives for floor tiles and wall coverings | 100 (in bitumen matrix) |
| Flooring | Thermoplastic floor tiles PVC vinyl floor tiles and unbacked sheet Asbestos paper-backing to PVC floor tiles | 25 7 100 |
| Reinforced plastic and resin composites | Toilet cisterns, seats, banisters | 1-10 |
| Other | Asbestos is such a versatile material that not all of its uses are known. It is sometimes found in obscure, unexpected places. |